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SECTION 09 90 00
PAINTS and COATINGS

MASTER
ARCHITECTURAL PAINTING SPECIFICATION
(Parallel Version – PPG - BM)



The information contained in this Behr Parallel Specification is primarily intended for use in reviewing commercial painting specification submittals. Because coating manufactures may change product formulations, users of this comparative data assume all responsibilities for acceptability of references such as resin types, composition, or gloss levels contained herein. Due to the many variables of Architects’ project painting specifications, it is recommended that the paint manufacturer(s) be contacted for their product’s intended use, technical data, (M)SDS and VOC content compliance with authorities having jurisdiction.
These BEHR PAINTS are in conformance with LEED v4 BUILDING DESIGN AND CONSTRUCTION for LEED v4 BD+C New Construction, Core and Shell, Schools, Retail, Hospitality and Healthcare. All Behr Paints comply with South Coast AQMD Rule 1113. Interior and other Behr Paints are GREENGUARD® Gold Certified.
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1801 E. St. Andrew Place, Santa Ana, California 92705 (714) 545-7101
**  NOTE TO SPECIFIER	This Section is for the specification of coatings in a mild to moderate environment.  It does contain some products from Diamond Vogel’s High Performance product lines to allow for design flexibility.  Diamond Vogel recommends the use of Section 09 96 00 High Performance Coatings for areas that require maximum protection. 
PART 1 - GENERAL
1.01 SUMMARY
Work includes furnishing of materials and equipment, preparation of surfaces and completion of painting and finishing of surfaces as required by Drawings and specified herein.
1.02 RELATED WORK
A. Factory, pre-finished items as specified in various sections.
B. Shop painting specified in respective sections.
C. Architectural woodworking.
D. Surfaces not to be painted:
1. Pre-finished wall, ceiling, and floor coverings.
2. Items with factory-applied final finish.
3. Concealed ducts, pipes, and conduit.
4. Surfaces specifically scheduled or noted on Drawings not to be painted. 
1.03 SUBMITTALS
A. Product data:
1. Not less than thirty (30) days before beginning work, submit a complete list of materials proposed for use, together with manufacturer's specifications.
2. Paint materials and products shall be subject to Architect's approval. 
B. Color samples: 
1. Prepare color and finishes on samples, 8-1/2" x 11" in size.
2. Submit samples as requested until required sheen, color and texture is achieved.
3. Prepare wood samples on type and quality of wood specified for use on project.
4. Label and identify each sample as to location and application. 

1.04 COLORS
A. Colors are to be selected or approved by Architect and actual color chips shall be supplied to Contractor for matching. All undercoats shall be tinted to approximately half the color of finish coat.
B. Approval of final colors: Do not apply final coat of paint until colors have been approved by Architect.
C. The number of colors to be used shall be as determined by Architect. Architect reserves right to vary colors throughout project. 
1.05 DELIVERY, STORAGE AND HANDLING
A. Deliver paint materials in sealed original labeled containers bearing manufacturer's name, type of paint, stock number, color, and instructions for reducing or mixing where applicable.
B. Paint materials and equipment
1. Store only acceptable project materials on site.
2. Store in a suitable location.
3. Restrict storage to paint materials and related materials.
4. Comply with health and fire regulations.
1.06 PROJECT CONDITIONS
A. Comply with manufacturer's recommendations as to environmental conditions under which coatings and coating systems can be applied. Do not apply paint or coatings when temperature is below 50F. Do not apply exterior paint in damp or rainy weather; ensure that the surface has dried thoroughly before proceeding.  Surface temperature must be at least 5°F above dew point before painting.
B. Do not apply finish in areas where dust or contaminants are being generated.

PART 2 - PRODUCTS
2.01 MATERIALS
A. Basis-of-Design Product: Provide products listed from Behr Paint Company, Santa Ana, California 92705, or comparable products by one of the following. Other manufacturers to conform to materials listed and be approved by Architect.
1. Sherwin-Williams Company
2. Benjamin Moore & Company
B. Materials selected for coating systems for each type of surface shall be the product of a single manufacturer.
C. Accessory materials such as thinner, linseed oil, putty and shellac shall be of the highest quality and by approved manufacturer, which comply with local VOC content limit regulations.
D. Paints shall be ready-mixed except field catalyzed coatings. 
E. Do not thin finish coats without Architect's approval.
F. Unsuitability of specified products: Claims concerning unsuitability of any material specified or inability to satisfactorily produce the work will not be entertained, unless such claim is made in writing to Architect before work is started.
G. Number of coats scheduled is minimum. Apply additional coats at no additional cost if necessary to completely hide base materials, produce uniform color and provide satisfactory finish result.
H. Submitted paints and coating shall comply with current local, state, and federal air quality regulations.
PART 3 - EXECUTION
3.01 EXAMINATION
A. Examine surfaces scheduled to receive paint and finishes for conditions that will adversely affect execution, permanence, or quality of work and which cannot be put into acceptable condition through preparatory work as included in Article 3.02 "Preparation ". Notify Owner’s Representative in writing of any defects or conditions which will prevent a satisfactory installation.
B. Examine surfaces scheduled to be finished prior to commencement of work. Report any condition that may potentially effect proper application.
C. Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows.
a. Concrete: 12 percent
b. Portland Cement Plaster and Stucco: 12 percent
c. Masonry (Clay and CMU): 12 percent
d. Wood: 15 percent
e. Gypsum Board: 12 percent
D. Portland Cement Plaster Substrates: Verify that plaster is fully cured.
E. Verify suitability of substrates, including surface conditions and compatibility with existing finishes and primers. 
F. Proceed with surface preparation and coating application only after unsatisfactory conditions have been corrected.
1. Application of coating is construed as acceptance of surfaces and conditions. 
3.02 PREPARATION 
A. Clean surfaces to receive paint thoroughly of substances, which could impair adhesion of paints, including dust, dirt, oil, and grease before application of any coatings. Prepare surfaces as follows:
1. WOOD SUBSTRATES: Remove mill glaze and dust, sand smooth. Fill open joints, cracks, nail holes and other pits or depressions flush and smooth with wood filler after priming. Use wood putty to match finish paint coat. Touch up knots or sap streaks with a stain-blocking sealer before priming.
2. CONCRETE, PRE-CAST CONCRETE, TILT-UP: Remove release agents, curing compounds, loose particles, efflorescence, and chalk.  Do not coat surfaces if moisture content or alkalinity of surface to be coated exceeds that permitted in the manufacturer’s written instructions. Prime with an alkali-resistant primer.
3. PLASTER and STUCCO SUBSTRATES: Fill hairline cracks, small holes, and imperfections on surfaces with patching compound. Smooth off to match adjacent surfaces. Apply an alkali-resistant primer or wash with fresh water and neutralize high alkalinity surfaces where they occur. 
4. MASONRY SUBSTRATES: Remove efflorescence and chalk. Do not coat surfaces if moisture content or alkalinity of surface to be coated exceeds that permitted in the manufacturer’s written instructions. Prime with an alkali-resistant primer.
5. SHOP-PRIMED STEEL SUBSTRATES: Solvent clean according to SSPC-SP1. Remove loose primer and rust, contaminants, and foreign matter. Prime bare steel and touch up abrasions with a ferrous metal primer.
6. STEEL, FERROUS METAL SUBSTRATES: Remove rust, mill scale, foreign substances, and shop primer. Clean according to SSPC-SP3, “Power Tool Cleaning”, or abrasive blasting cleaning according to SSPC-SP6 “Commercial Blast Cleaning” as required. Protect surface from corrosion until application of primer.
7. GALVANIZED METAL: Remove oils, passivators and clean entire surface with an appropriate solvent. Pre-treat with a phosphoric acid etching solution to promote adhesion of subsequently applied coatings.
8. PHOSPHATIZED METAL or GALVANNEALED METAL shall not be chemically etched. Clean and apply suitable metal primer.
9. ALUMINUM SUBSTRATES: Solvent clean according to SSPC-SP1. Remove loose surface oxidation.
10. GYPSUM BOARD SUBSTRATES: Remove dust and foreign matter. Fill pits flush and smooth with joint compound and where required, apply skim coat to provide the required finishing level based on GA-214-96, Recommended Levels of Gypsum Board Finish before application of decoration.
B. Surfaces, which cannot be prepared or painted as specified, shall be immediately brought to attention of Architect in writing.
1. Starting of work without such notification will be considered acceptance by the Contractor of surfaces involved.
2. Replace unsatisfactory work caused by improper or defective surfaces as directed by Architect at no additional cost to Owner. 
3.03 APPLICATION
A. Do not apply initial coating until moisture content of surface is within limitations recommended by paint manufacturer.
B. Application:
1. Apply paint with suitable brushes, rollers or spraying equipment.
2. Apply stain in accordance with manufacturer's recommendations.
3. Rate of application shall not exceed that as recommended by paint manufacturer for surface involved. 
C. Comply with recommendations of product manufacturer for drying time between succeeding coats.
D. Leave parts of molding and ornaments clean and true to details with no undue amount of paint in corners and depressions.
E. Make edges of paint adjoining other material or color clean and sharp with no overlapping.
F. Refinish whole wall where portion of finish is not acceptable.
G. Apply materials evenly with proper film thickness and free of runs, sags, skips and other defects. Hard, glossy finishes shall be sanded lightly between coats, dusted, and cleaned before recoating.
H. Remove hardware, hardware accessories, plates, lighting fixtures and similar items in place prior to painting and replaced upon completion of each space.
I. Disconnect heating and other equipment adjacent to walls using workmen skilled in appropriate trades, and moved to permit wall surfaces to be painted. Following completion of painting, they shall be expertly replaced and reconnected.
J. Paint visible surfaces behind vents, registers, or grilles flat black.
1. Wash exposed metal with solvent then prime and paint as scheduled.
2. Spray paint wherever practical. 
K. Do not paint over Underwriters' labels, fusible links, or sprinkler heads.
L. EXPOSED PLUMBING AND MECHANICAL ITEMS: Items without factory finish such as conduits, pipes, access panels and items of similar nature shall be finished to match adjacent wall and ceiling surfaces unless otherwise directed. 
3.04 CLEANUP
Upon completion of work, remove equipment, excess material, and debris, remove paint splatters, and leave area in a neat and orderly condition.
3.05 PROTECTION
A. Protect work of other trades, whether to be painted or not, against damage by painting. Correct damage by cleaning, repairing, or replacing, and repainting, as acceptable to Architect.
B. Provide "wet paint" signs to protect newly painted finishes. Remove temporary protective wrappings provided by others for protection of their work after completion of painting operations.
1. At completion of construction activities of other trades, touch up and restore damaged or   defaced painted surfaces.
3.06 FINISH SCHEDULE
A. Finish surfaces in accordance with schedule. Catalog names and numbers refer to products as manufactured by the Behr Paint Company, Santa Ana, California 92705, except as otherwise specified. 
B. Provide paint finishes of even uniform color, free from cloudy or mottled appearance. Properly correct non- complying work to satisfaction of Owner’s representative and representative of Behr Process Corporation.

C. Some colors, especially accent colors may require multiple finish coats for adequate coverage and opacity.

D. The specified number of primer and finish coats is minimum acceptable. If full coverage and opacity is not obtained with specified number of coats, apply additional coats as necessary to produce required finish. 

E. Application Finish Schedule:

EXTERIOR PAINT SCHEDULE:



			
	BEHR
	PPG Paints
	Benjamin Moore



1. Stucco, Cement Plaster
Flat – Premium Exterior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Premium Plus Exterior Flat 4050
	Sun Proof Latex Flat 72-45XI
	Moorlife Acrylic Flat N105

	Topcoat:
	Premium Plus Exterior Flat 4050
	Sun Proof Flat Latex 72-45XI
	Moorlife Acrylic Flat N105



	 Satin – Premium Exterior 100% Acrylic	
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Premium Plus Exterior Satin 9050
	Sun Proof Latex Satin 76-45XI
	Moorgard Low Lustre N103

	Topcoat:
	Premium Plus Exterior Satin 9050
	Sun Proof Latex Satin 76-45XI
	Moorgard Low Lustre N103



	Semi-Gloss – Premium Exterior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XIXI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss 78-45XI
	Moorglo Soft Gloss N096

	Topcoat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss 78-45XI
	Moorglo Soft Gloss N096



Flat – Professional Exterior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XIXI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Exterior Flat 6-610XI
	Ultra Spec Ext Flat N447 

	Topcoat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Exterior Flat 6-610XI
	Ultra Spec Ext Flat N447 



	Satin – Professional Exterior 100% Acrylic	
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XIXI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2045XI
	Ultra Spec Ext Satin N448

	Topcoat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2045XI
	Ultra Spec Ext Satin N448



	Semi-Gloss – Professional Exterior 100% Acrylic	
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XIXI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-900XI
	Ultra Spec Ext Gloss N449

	Topcoat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-900XI
	Ultra Spec Ext Gloss N449



2. Stucco and Cement Plaster – High Build Coating
	Flat – Exterior High Build Coating 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XIXI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Premium Exterior High Build Coating 4700
	Perma-Crete High Build Acrylic 4-22
	Super Spec Masonry Coating 056

	Topcoat:
	Premium Exterior High Build Coating 4700
	Perma-Crete High Build Acrylic 4-22
	Super Spec Masonry Coating 056



3. [bookmark: _Hlk92803051]Stucco and Cement Plaster – Texture Coating
Flat Exterior Acrylic Texture Coating – Medium 
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XIXI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Exterior Acrylic Texture Coating - Medium PR710
	Perma-Crete Medium Texture Coating 4-60
	High Build Exterior Texture Medium Flat 437

	Topcoat:
	Exterior Acrylic Texture Coating -Medium PR710
	Perma-Crete Medium Texture Coating 4-60
	High Build Exterior Texture Medium Flat 437



4. Stucco, Cement Plaster, Masonry & Brick - Elastomeric
Exterior 100% Acrylic Elastomeric Coating
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Premium Exterior Elastomeric Paint 68
	Pitt-Flex Elastomeric 4-110 P-C
	Super Spec Elastomeric N055

	Topcoat:
	Premium Exterior Elastomeric Paint 68
	Pitt-Flex Elastomeric 4-110 P-C
	Super Spec Elastomeric N055


5. Concrete, Tilt-Up
	Flat – Exterior, Professional, 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Acrylic Flat 6-610XI
	Ultra Spec Ext Flat N447 

	Topcoat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Acrylic Flat 6-610XI
	Ultra Spec Ext Flat N447 




			BEHR
	PPG Paints
	Benjamin Moore



	Satin – Exterior, Professional, 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2045XI
	Ultra Spec Ext Satin N448

	Topcoat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2045XI
	Ultra Spec Ext Satin N448



	Semi-Gloss – Professional, Exterior 100% Acrylic 
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-900XI
	Ultra Spec Ext Gloss N449

	Topcoat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-900XI
	Ultra Spec Ext Gloss N449


6. Concrete Tilt-Up – Texture Coating
Flat Exterior Acrylic Texture Coating – Medium 
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XIXI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Exterior Acrylic Texture Coating - Medium PR710
	Perma-Crete Medium Texture Coating 4-60
	High Build Exterior Texture Medium Flat 437

	Topcoat:
	Exterior Acrylic Texture Coating -Medium PR710
	Perma-Crete Medium Texture Coating 4-60
	High Build Exterior Texture Medium Flat 437



7. Concrete Tilt-Up – High Build Coating
	Flat – Exterior High Build Coating 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Premium Exterior High Build Coating 4700
	Perma-Crete High Build Acrylic  4-22
	Super Spec Masonry Coating 056

	Topcoat:
	Premium Exterior High Build Coating 4700
	Perma-Crete High Build Acrylic  4-22
	Super Spec Masonry Coating 056



8. Concrete Tilt-Up – Elastomeric
	Exterior 100% Acrylic Elastomeric Coating
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Perma-Crete Primer 4-603XI
	Ultra Spec Masonry Sealer 608 

	Intermediate Coat:
	Premium Exterior Elastomeric Paint 68
	Pitt-Flex Elastomeric 4-110 C
	Super Spec Elastomeric 055

	Topcoat:
	Premium Exterior Elastomeric Paint 68
	Pitt-Flex Elastomeric 4-110 C
	Super Spec Elastomeric 055



9. Concrete Masonry Units (CMU)
Flat – Premium Exterior 100% Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XIXI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Plus Exterior Flat 4050
	Sun Proof Latex Flat 72-45XI
	Moorlife Acrylic Flat N105

	Topcoat:
	Premium Plus Exterior Flat 4050
	Sun Proof Latex Flat 72-45XI
	Moorlife Acrylic Flat N105



	Satin – Premium Exterior 100% Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XIXI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Plus Exterior Satin 9050
	Sun Proof Latex Satin 76-45XI
	Moorgard Low Lustre N103

	Topcoat:
	Premium Plus Exterior Satin 9050
	Sun Proof Latex Satin 76-45XI
	Moorgard Low Lustre N103



	Semi-Gloss – Premium Exterior 100% Acrylic 
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XIXI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss 78-45XI
	Moorglo Soft Gloss N096

	Topcoat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss 78-45XI
	Moorglo Soft Gloss N096



Flat – Exterior, Professional 100% Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XIXI
	Super Spec Block Filler 160

	Intermediate Coat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Acrylic Flat 6-610XI
	Ultra Spec Ext Flat N447 

	Topcoat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Acrylic Flat 6-610XI
	Ultra Spec Ext Flat N447 



	Satin – Exterior, Professional, 100% Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XIXI
	Super Spec Block Filler 160

	Intermediate Coat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2045XI
	Ultra Spec Ext Satin N448

	Topcoat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2045XI
	Ultra Spec Ext Satin N448



	BEHR
	PPG Paints
	Benjamin Moore



	Semi-Gloss – Professional, Exterior 100% Acrylic 
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-900XI
	Ultra Spec Ext Gloss N449

	Topcoat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-900XI
	Ultra Spec Ext Gloss N449



10. Concrete Masonry Units – Texture Coating
Flat Exterior Acrylic Texture Coating – Medium 
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Exterior Acrylic Texture Coating - Medium PR710
	Perma-Crete Medium Texture Coating 4-60
	High Build Exterior Texture Medium Flat 437

	Topcoat:
	Exterior Acrylic Texture Coating -Medium PR710
	Perma-Crete Medium Texture Coating 4-60
	High Build Exterior Texture Medium Flat 437


11. Concrete Masonry Units (CMU) - High Build Coating
	Flat – High Build Coating 100% Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium High Build Coating 4700
	Perma-Crete High Build Acrylic 4-22
	Super Spec Masonry Coating 056

	Topcoat:
	Premium High Build Coating 4700
	Perma-Crete High Build Acrylic 4-22
	Super Spec Masonry Coating 056



12. Concrete Masonry Units (CMU) - Elastomeric
Exterior 100% Acrylic Elastomeric Coating
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Exterior Elastomeric Paint 68
	Pitt-Flex Elastomeric 4-110 P-C
	Super Spec Elastomeric N055

	Topcoat:
	Premium Exterior Elastomeric Paint 68
	Pitt-Flex Elastomeric 4-110 P-C
	Super Spec Elastomeric N055



13. [bookmark: _Hlk92803475]Concrete Porch and Patio
Low Luster Exterior/Interior 100% Acrylic 
	Prime Coat: 
	Concrete Bonding Primer 880*
	Floor & Porch Satin 3-510XI
	Latex Floor & Patio N122

	Intermediate Coat:
	Porch/Patio Low Lustre Enamel 6050
	Floor & Porch Satin 3-510XI
	Latex Floor & Patio N122

	Topcoat:
	Porch/Patio Low Lustre Enamel 6050
	Floor & Porch Satin 3-510XI
	Latex Floor & Patio N122


Note *Intended for use on rough and porous concrete surfaces.

Gloss Exterior/Premium, Latex, Interior, Low Odor/VOC 
	Prime Coat:
	Concrete & Masonry Bonding Primer 880*
	Floor & Porch Gloss 6-510C
	Latex Floor & Patio Gloss 0121

	Intermediate Coat:
	Premium Porch/Patio Gloss Enamel 6705
	Floor & Porch Gloss 6-510C
	Latex Floor & Patio Gloss 0121

	Topcoat:
	Premium Porch/Patio Gloss Enamel 6705
	Floor & Porch Gloss 6-510C      
	Latex Floor & Patio Gloss 0121



Note* Intended for use on rough and porous concrete surfaces.

14. Anti-Slip Concrete Porch and Patio – Low Luster
Anti-Slip Low Luster Exterior/Interior 100% Acrylic 
	Prime Coat: 
	Concrete Bonding Primer 880*
	N/A
	N/A

	Intermediate Coat:
	Porch/Patio Anti-Slip Floor Paint 6250
	N/A
	N/A

	Topcoat:
	Porch/Patio Anti-Slip Floor Paint 6250
	N/A
	N/A


Note *Intended for use on rough and porous concrete surfaces.

15. Concrete, Decks, Walkways, Pool Decks and Sidewalks – Solid Color Coating
Flat – Premium Exterior Solid Color Coating, 100% Acrylic 
	Prime Coat: 
	Behr Premium DeckOver 5000
	N/A
	N/A

	Topcoat:
	Behr Premium DeckOver 5000
	N/A 
	N/A



16. Concrete, Decks, Walkways, Pool Decks and Sidewalks – Textured Solid Color Coating
Flat – Premium Exterior Solid Color Coating, 100% Acrylic 
	Prime Coat:
	Behr Textured DeckOver Solid Color Coating 5005
	N/A
	N/A

	Topcoat:
	Behr Textured DeckOver Solid Color Coating 5005
	N/A 
	N/A





	BEHR
	PPG Paints
	Benjamin Moore



17. Wood, Paint Finish
Flat – Premium Exterior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Exterior Flat 4050
	Sun Proof Exterior Flat 72-110XI
	Moorlife Acrylic Flat N105

	Topcoat:
	Premium Plus Exterior Flat 4050
	Sun Proof Exterior Flat 72-110XI
	Moorlife Acrylic Flat N105



	Satin – Premium Exterior 100% Acrylic	
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Exterior Satin 9050
	Sun Proof Satin Latex 76-110XI
	Moorgard Low Lustre N103

	Topcoat:
	Premium Plus Exterior Satin 9050
	Sun Proof Satin Latex 76-110XI
	Moorgard Low Lustre N103


	
	Semi-Gloss – Premium Exterior 100% Acrylic 
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss Latex 78-110XI
	Moorglo Soft Gloss N096

	Topcoat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss Latex 78-110XI
	Moorglo Soft Gloss N096



	Gloss – Premium Exterior 100% Acrylic 
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Int/Ext Hi-Gloss 8050
	Advantage 900  Gloss 909-10
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Int/Ext Hi-Gloss 8050
	Advantage 900  Gloss 909-10
	Impervex Latex Gloss W309


 (Note: * 2-8050 Hi-Gloss Enamel conforms to VOC content limits of South Coast AQMD Rule 1113.)

Flat – Exterior, Professional 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro e600 Exterior Flat PR610
	Speedhide Acrylic Flat 6-650XI
	Ultra Spec Ext Flat N447 

	Topcoat:
	Behr Pro e600 Exterior Flat PR610
	Speedhide Acrylic Flat 6-650XI
	Ultra Spec Ext Flat N447 



	Satin – Exterior, Professional, 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro e600 Exterior Satin PR640
	Speedhide Ext. Satin 6-2110XI
	Ultra Spec Ext Satin N448

	Topcoat:
	Behr Pro e600 Exterior Satin PR640
	Speedhide Ext. Satin 6-2110XI
	Ultra Spec Ext Satin N448



	Semi-Gloss – Professional, Exterior 100% Acrylic 
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-901XI
	Ultra Spec Ext Gloss N449

	Topcoat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-901XI
	Ultra Spec Ext Gloss N449


18. Wood, Paint Finish – Urethane Alkyd, Water-Reducible and Alkyd Waterborne
	Semi-Gloss – Interior / Exterior Enamel
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	N/A

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd SG 6-1510XI
	N/A

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900 
	Speedhide WB Alkyd SG 6-1510XI
	N/A



	Satin – Interior / Exterior Enamel
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Seal Grip Primer & Sealer 17-921
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Urethane Alkyd Satin  Enamel 7900
	Speedhide WB Alkyd Satin 6-1410XI
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin  Enamel 7900
	Speedhide WB Alkyd Satin 6-1410XI
	Aura Grand Entrance Satin 147



19. Wood, Stain Finish, Water-Based, Semi-Transparent
	Flat – 100% Acrylic
	Two Coats:
	Semi-Transparent Stain, Waterproofer
	Proluxe SRD Semi-Transparent 
	 Arborcoat WB S/T Stain 638

	Or - Two Coats:
	Sealer 5077, Redwood S/T Stain 5330
	Wood Finish AKN00015
	

	Or – Two Coats
	Cedar Naturaltone S/T Stain 5533
	
	


	
20. Wood, Stain Finish, Water-Based, Solid Color
	Flat – 100% Acrylic
	Two Coats:
	Solid Color Stain & Waterproofer White 5011, Deep Base 5013
	Proluxe Premium Solid Color Wood Finish SIK710-100
	Arborcoat Solid Color Stain 640

	Or – Two Coats
	Cedar Naturaltone S/T Stain 50533
	
	




	BEHR
	 PPG Paints
	           Benjamin Moore




21. Wood, Wood Composite – Decks, Patios, Boat Docks, Railings – Solid Color Coating
	Flat – 100% Acrylic, Solid Color Coating
	[bookmark: _Hlk92805683]Two Coats:
	DeckOver Solid Color Coating 5000
	N/A
	N/A



22. Wood, Wood Composite – Decks, Patios, Boat Docks, Railings – Texture Solid Color Coating
Flat – 100% Acrylic, Solid Color Textured Coating
	Two Coats:
	Advanced DeckOver Texture Coating 5005
	N/A
	N/A


	
23. Steel, Ferrous Metal
Flat – Premium Exterior 100% Acrylic
	Prime Coat:
	Behr Interior/Exterior Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Acrylic Metal Primer M04

	Intermediate Coat:
	Premium Plus Exterior Flat 4050
	Sun Proof Exterior Flat 72-110XI
	Moorlife Acrylic Flat N105

	Topcoat:
	Premium Plus Exterior Flat 4050
	SunProof Exterior Flat 72-110XI
	Moorlife Acrylic Flat N105



	 Satin – Premium Exterior 100% Acrylic	
	Prime Coat:
	Behr Interior/Exterior Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Acrylic Metal Primer M04

	Intermediate Coat:
	Premium Plus Exterior Satin 9050
	Sun Proof Satin Latex 76-110XI
	Moorgard Low Lustre W103

	Topcoat:
	Premium Plus Exterior Satin 9050
	Sun Proof Satin Latex 76-110XI
	Moorgard Low Lustre W103


	
Semi-Gloss – Premium Exterior 100% Acrylic 
	Prime Coat:
	Behr Interior/Exterior Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Acrylic Metal Primer M04

	Intermediate Coat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss Latex 78-110XI
	Moorglo Soft Gloss N096

	Topcoat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss Latex 78-110XI
	Moorglo Soft Gloss N096



Gloss – Premium Exterior 100% Acrylic 
	Prime Coat:
	Behr Interior/Exterior Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Acrylic Metal Primer M04

	Intermediate Coat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Advantage 900  Gloss 909-10
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Advantage 900  Gloss 909-10
	Impervex Latex Gloss W309



Flat – Exterior, Professional 100% Acrylic
	Prime Coat:
	Behr Interior/Exterior Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Acrylic Metal Primer M04

	Intermediate Coat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Acrylic Flat 6-650XI
	Ultra Spec Ext Flat N447

	Topcoat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Acrylic Flat 6-650XI
	Ultra Spec Ext Flat N447



	Satin – Exterior, Professional, 100% Acrylic
	Prime Coat:
	Behr Interior/Exterior Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Acrylic Metal Primer M04

	Intermediate Coat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2110XI
	Ultra Spec Ext Satin N448

	Topcoat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2110XI
	Ultra Spec Ext Satin N448



	Semi-Gloss – Professional, Exterior 100% Acrylic 
	Prime Coat:
	Behr Interior/Exterior Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Acrylic Metal Primer M04

	Intermediate Coat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-901XI
	Ultra Spec Ext Gloss N449

	Topcoat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-901XI
	Ultra Spec Ext Gloss N449



24. Steel, Ferrous Metal – Urethane Alkyd, Water-Reducible and Alkyd Waterborne
	Semi-Gloss – Interior / Exterior Enamel
	Prime Coat:
	Behr Interior/Exterior Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	N/A

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd Semi-Gloss 6-1510XI
	N/A

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd Semi-Gloss 6-1510XI
	N/A


	
	Satin – Interior / Exterior Enamel
	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Satin 6-1410XI
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Satin 6-1410XI
	Aura Grand Entrance Satin 147



25. Steel, Ferrous Metal – High Performance, Water-Based, Industrial Maintenance 
	Semi-Gloss, 100% Acrylic, Direct-To-Metal Enamel
	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Direct-To-Metal Semi-Gloss 3200
	Pitt-Tech Plus Semi-Gloss DTM 90-1210
	Super Spec DTM Semi-Gloss P29

	Topcoat:
	Direct-To-Metal Semi-Gloss 3200
	Pitt-Tech Plus Semi-Gloss DTM 90-1210
	Super Spec DTM Semi-Gloss P29






	BEHR
	PPG Paints
	    Benjamin Moore







	Gloss, 100% Acrylic, Direct-To-Metal Enamel
	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Direct-To-Metal Gloss 8200
	Pitt-Tech Plus Gloss DTM 90-1310
	Super Spec HP DTM Acrylic Gloss P28

	Topcoat:
	Direct-To-Metal Gloss 8200
	Pitt-Tech Plus Gloss DTM 90-1310
	Super Spec HP DTM Acrylic Gloss P28



26. Galvanized Metal, Aluminum, and Non-Ferrous Metals
Flat – Exterior 100% Acrylic
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Exterior Flat 4050
	Sun Proof Exterior Flat 72-110XI
	Moorlife Acrylic Flat N105

	Topcoat:
	Premium Plus Exterior Flat 4050
	Sun Proof Exterior Flat 72-110XI
	Moorlife Acrylic Flat N105



	Satin – Exterior 100% Acrylic	
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Exterior Satin 9050
	Sun Proof Satin Latex 76-110XI
	Moorgard Low Lustre W103

	Topcoat:
	Premium Plus Exterior Satin 9050
	Sun Proof Satin Latex 76-110XI
	Moorgard Low Lustre W103



	Semi-Gloss – Exterior 100% Acrylic 
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Exterior Semi-Gloss 5050 
	Sun Proof Semi-Gloss 78-110Xi
	Moorglo Soft Gloss N096

	Topcoat:
	Premium Plus Exterior Semi-Gloss 5050
	Sun Proof Semi-Gloss 78-110XI
	Moorglo Soft Gloss N096



	Gloss – Exterior 100% Acrylic 
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Advantage 900  Gloss 909-10
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Advantage 900  Gloss 909-10
	Impervex Latex Gloss W309



Flat – Exterior, Professional 100% Acrylic
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Acrylic Flat 6-650XI
	Ultra Spec Ext Flat N447

	Topcoat:
	Behr Pro e600 Exterior Flat PR 610
	Speedhide Acrylic Flat 6-650XI
	Ultra Spec Ext Flat N447



	Satin – Exterior, Professional, 100% Acrylic
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2110XI
	Ultra Spec Ext Satin N448

	Topcoat:
	Behr Pro e600 Exterior Satin PR 640
	Speedhide Ext. Satin 6-2110XI
	Ultra Spec Ext Satin N448


	Semi-Gloss – Professional, Exterior 100% Acrylic 
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-901XI
	Ultra Spec Ext Gloss N449

	Topcoat:
	Behr Pro e600 Exterior Semi-Gloss PR670
	Speedhide Ext. Semi-Gloss 6-901XI
	Ultra Spec Ext Gloss N449



27. Galvanized Metal, Aluminum, Non-Ferrous Metals - Urethane Alkyd, Water-Reducible and Alkyd Waterborne
	Semi-Gloss – Interior / Exterior Enamel
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	N/A

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	N/A

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd Semi-Gloss 6-1510XI
	N/A

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900 
	Speedhide WB Alkyd Semi-Gloss 6-1510XI
	N/A



	Satin – Interior / Exterior Enamel
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Satin 6-1410XI
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Satin 6-1410XI
	Aura Grand Entrance Satin 147




	                  BEHR
	      PPG Paints
	       Benjamin Moore


 
28. Galvanized Metal, Aluminum, Non-Ferrous Metals – High Performance, Industrial Maintenance 
	Semi-Gloss, 100% Acrylic, Direct-To-Metal Enamel
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Direct-To-Metal Semi-Gloss 3200
	Pitt-Tech Plus Semi-Gloss DTM 90-1210
	Super Spec HP DTM Semi-Gloss P29

	Topcoat:
	Premium Direct-To-Metal Semi-Gloss 3200
	Pitt-Tech Plus Semi-Gloss DTM 90-1210
	Super Spec HP DTM Semi-Gloss P29



	Gloss, 100% Acrylic, Direct-To-Metal Enamel
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended
	Krud Kutter Metal Clean & Etch 

	Prime Coat:
	Behr Int/Ext Metal Primer 435
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer M04

	Intermediate Coat:
	Direct-To-Metal Gloss 8200
	Pitt-Tech Plus Gloss DTM 90-1310
	Super Spec DTM Acrylic Gloss P28

	Topcoat:
	Direct-To-Metal Gloss 8200
	Pitt-Tech Plus Gloss DTM 90-1310
	Super Spec DTM Acrylic Gloss P28



INTERIOR PAINT SCHEDULE

1. Gypsum Board
Flat – Premium Interior, Acrylic
	Prime Coat:
	Behr Drywall Primer & Sealer 73
	Pure Performance Primer 9-900
	Ultra Spec Latex Primer N534

	Intermediate Coat:
	Premium Plus Interior Flat 1050
	Pure Performance Flat 9-110XI
	Regal Select Flat 547

	Topcoat:
	Premium Plus Interior Flat 1050
	Pure Performance Flat 9-110XI
	Regal Select Flat 547



Eggshell – Premium Interior, Acrylic
	Prime Coat:
	Behr Drywall Primer & Sealer 73
	Pure Performance Primer 9-900
	Ultra Spec Latex Primer N534

	Intermediate Coat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 9-310XI
	Regal Select Eggshell 549

	Topcoat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 9-310XI
	Regal Select Eggshell 549



Satin – Premium Interior, Acrylic
	Prime Coat:
	Behr Drywall Primer & Sealer 73
	Pure Performance Primer 9-900
	Ultra Spec Latex Primer N534

	Intermediate Coat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-3410
	Regal Select Pearl 550

	Topcoat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-3410
	Regal Select Pearl 550



Semi-Gloss – Premium Interior, Acrylic
	Prime Coat:
	Behr Drywall Primer & Sealer 73
	Pure Performance Primer 9-900
	Ultra Spec Latex Primer N534

	Intermediate Coat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance Semi-Gloss         9-510XI
	Regal Select Semi-Gloss 551

	Topcoat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance Semi-Gloss         9-510XI 
	Regal Select Semi-Gloss 551



Gloss – Premium Interior, Acrylic
	Prime Coat:
	Behr Drywall Primer & Sealer 73
	Pure Performance Primer 9-900
	Ultra Spec Latex Primer N534

	Intermediate Coat:
	Premium Plus Int/Ext Hi-Gloss 2-8050
	Advantage 900 Gloss 909-10
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Int/Ext Hi-Gloss 2-8050
	Advantage 900 Gloss 909-10
	Impervex Latex Gloss W309









Flat – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Kilz PVA Drywall Interior Primer & Sealer PX010
	Speedhide Zero Interior Latex Sealer 6-4900XI
	Ultra Spec Latex Primer 534

	Intermediate Coat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110XI
	Ultra Spec 500 Int. Flat 536

	Topcoat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110XI
	Ultra Spec 500 Int. Flat 536



Eggshell – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Kilz PVA Drywall Interior Primer & Sealer PX010
	Speedhide Zero Interior Latex Sealer        6-4900XI
	Ultra Spec Latex Primer 534

	Intermediate Coat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell 6-4310XI
	Ultra Spec 500 Eggshell 538

	Topcoat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell 6-4310XI
	Ultra Spec 500 Eggshell 538



Semi-Gloss – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Kilz PVA Drywall Interior Primer & Sealer PX010
	Speedhide Zero Interior Latex Sealer 6-4900XI
	Ultra Spec Latex Primer 534

	Intermediate Coat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss 6-4510XI
	Ultra Spec 500 Semi-Gloss 539

	Topcoat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss 6-4510XI
	Ultra Spec 500 Semi-Gloss 539



2. Gypsum Board: High Performance Coating
	Eggshell – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Premium Plus All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 



Semi-Gloss – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Premium Plus All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss



3. Gypsum Board – Urethane Alkyd, Water-Reducible and Alkyd Waterborne
	Semi-Gloss – Interior / Exterior Enamel
	Prime Coat:
	Behr Drywall Primer & Sealer 73
	Pure Performance Primer 9-900
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd Semi-Gloss 6-1510
	Advance Waterborne Alkyd Semi-Gloss 793

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900 
	Speedhide WB Alkyd Semi-Gloss 6-1510
	Advance Waterborne Alkyd Semi-Gloss 793


	Satin – Interior / Exterior Enamel
	Prime Coat:
	Behr Drywall Primer & Sealer 73
	Pure Performance Primer 9-900
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Satin 6-1410
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Satin 6-1410
	Aura Grand Entrance Satin 147



4. Gypsum Board - Ceilings
Flat – Interior, Acrylic
	Prime Coat:
	Kilz PVA Drywall Primer & Sealer PX010
	Speedhide Zero Interior Latex Sealer 6-4900XI
	Ultra Spec Latex Primer N534

	Intermediate Coat:
	Interior Ceiling Flat 5558
	Ceiling Paint Flat Latex 17-45
	Muresco Ceiling White 258

	Topcoat:
	Interior Ceiling Flat 5558
	Ceiling Paint Flat Latex 17-45
	Muresco Ceiling White 258







			BEHR
	PPG Paints
	       Benjamin Moore


5. Gypsum Board - Dry Fall Coating (Spray Applied)
Flat – Interior, Acrylic, Spray Applied
	Prime Coat:
	Kilz PVA Drywall Primer & Sealer PX010
	Speedhide Zero Interior Latex Sealer 6-4900XI
	Ultra Spec Latex Primer N534

	Intermediate Coat:
	Behr Pro 890 White, 891 Black Dryfall Flat
	Speedhide Dry-Fog Flat 6-275Xl 
	Sweep Up Latex Flat 153

	Topcoat:
	Behr Pro 890 White, 891 Black Dryfall Flat
	Speedhide Dry-Fog Flat 6-275Xl
	Sweep Up Latex Flat 153



6. Concrete, Plaster, Masonry
Flat – Premium Interior, Acrylic
	Prime Coat:
	Premium All-In-One Primer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat 547

	Topcoat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat 547



Eggshell – Premium Interior, Acrylic
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell                                                                                                                           9-300Xl
	Regal Select Eggshell 549

	Topcoat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 9-300Xl
	Regal Select Eggshell 549



Satin – Premium Interior, Acrylic
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550

	Topcoat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550



	Semi-Gloss – Premium Interior, Acrylic
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance  Semi-Gloss 
9-500Xl
	Regal Select Semi-Gloss 551

	Topcoat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance  Semi-Gloss 
9-500Xl
	Regal Select Semi-Gloss 551



Gloss – Premium Interior, Acrylic
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Premium Plus Hi-Gloss 2-8050
	Manor Hall Gloss 52-110
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Hi-Gloss 2-8050
	Manor Hall Gloss 52-110
	Impervex Latex Gloss W309



Flat – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536

	Topcoat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536



Eggshell – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell 6-4310XI
	Ultra Spec 500 Eggshell 538

	Topcoat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell 6-4310XI
	Ultra Spec 500 Eggshell 538



Semi-Gloss – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss 539

	Topcoat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss 539


	
7. Concrete, Plaster, Masonry: Light Industrial Coating
	Eggshell – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 






			BEHR
	PPG Paints
	     Benjamin Moore


Semi-Gloss – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Premium Plus All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss 


8. Concrete, Plaster, Masonry – Urethane Alkyd, Water-Reducible and Alkyd Waterborne 
	Semi-Gloss – Interior / Exterior Enamel
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd SG 6-1510
	Advance Waterborne Alkyd Semi-Gloss 793

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900 
	Speedhide WB Alkyd SG 6-1510
	Advance Waterborne Alkyd Semi-Gloss 793



	Satin – Interior / Exterior Enamel
	Prime Coat:
	All-In-One Primer Sealer 75
	Perma-Crete Primer 4-603XI
	Fresh Start Latex Primer N023

	Intermediate Coat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Semi-Gloss 6-1410
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Semi-Gloss 6-1410
	Aura Grand Entrance Satin 147



9. Concrete Porches and Patios
Low Luster Exterior/Interior 100% Acrylic 
	Prime Coat:
	880 Concrete Bonding Primer*
	Floor & Porch Satin Latex 3-510
	Latex Floor & Patio N122

	Intermediate Coat:
	Premium Porch/Patio Enamel 6050
	Floor & Porch Satin Latex 3-510
	Latex Floor & Patio N122

	Topcoat:
	Premium Porch/Patio Enamel 6050
	Floor & Porch Satin Latex 3-510
	Latex Floor & Patio N122


	
Note* Intended for use on rough, porous concrete.
Gloss Exterior/Premium, Latex, Interior, Low Odor/VOC 
	Prime Coat:
	Concrete & Masonry Bonding Primer 880* 
	N/A
	Latex Floor & Patio Gloss 0121

	Intermediate Coat:
	Premium Porch/Patio Gloss Enamel 6700
	N/A
	Latex Floor & Patio Gloss 0121

	Topcoat:
	Premium Porch/Patio Gloss Enamel 6700
	N/A
	Latex Floor & Patio Gloss 0121



Note* Intended for use on rough, porous concrete.

10. Concrete Masonry Units (CMU)
Flat – Premium Interior, Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50 
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat 547

	Topcoat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat 547



Eggshell – Premium Interior, Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 9-300Xl 
	Regal Select Eggshell 549

	Topcoat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 9-300Xl
	Regal Select Eggshell 549


Satin – Premium Interior, Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550

	Topcoat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550



	Semi-Gloss – Premium Interior, Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance Semi-Gloss 9-500Xl
	Regal Select Semi-Gloss 551

	Topcoat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance Semi-Gloss 9-500Xl
	Regal Select Semi-Gloss 551


	Gloss – Premium Interior, Acrylic
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Manor Hall Gloss 52-110
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Manor Hall Gloss 52-110
	Impervex Latex Gloss W309




			BEHR
	PPG Paints
	   Benjamin Moore


Flat – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536

	Topcoat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536



Eggshell – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell 6-4310XI
	Ultra Spec 500 Eggshell 538

	Topcoat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell 6-4310XI
	Ultra Spec 500 Eggshell 538



Semi-Gloss – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss N539

	Topcoat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss N539


	
11. Concrete Masonry Units (CMU): Light Industrial Coating
	Eggshell – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 



	Semi-Gloss – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss



12. Concrete Masonry Units – Urethane Alkyd, Water-Reducible and Alkyd Waterborne
	Semi-Gloss – Interior / Exterior Enamel
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd SG 6-1510
	Advance Waterborne Alkyd 793

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900 
	Speedhide WB Alkyd SG 6-1510
	Advance Waterborne Alkyd 793



	Satin – Interior / Exterior Enamel
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Block Filler 160

	Intermediate Coat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Semi-Gloss 6-1410
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Semi-Gloss 6-1410
	Aura Grand Entrance Satin 147



13. Steel, Ferrous Metal
Flat – Premium Interior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Acrylic Metal Primer M04

	Intermediate Coat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat K547

	Topcoat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat K547


	
Eggshell – Premium Interior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 9-300Xl
	Regal Select Eggshell 549

	Topcoat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 9-300Xl
	Regal Select Eggshell 549



Satin – Premium Interior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550

	Topcoat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550



			BEHR
	PPG Paints
	Benjamin Moore


Semi-Gloss – Premium Interior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance Eggshell 9-300Xl
	Regal Select Semi-Gloss 551

	Topcoat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance Eggshell 9-300Xl
	Regal Select Semi-Gloss 551



Gloss – Premium Interior 100% Acrylic
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer p04

	Intermediate Coat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Pure Performance  Semi-Gloss 
9-500Xl
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Pure Performance  Semi-Gloss 
9-500Xl
	Impervex Latex Gloss W309



Flat – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536

	Topcoat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536



Eggshell – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell         6-4310XI
	Ultra Spec 500 Eggshell 538

	Topcoat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell         6-4310XI
	Ultra Spec 500 Eggshell 538



Semi-Gloss – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss N539

	Topcoat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss N539



14. Steel, Ferrous Metal – Light Industrial Coatings
	Eggshell – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 



	Semi-Gloss – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss


	
15. Steel, Ferrous Metal – Urethane Alkyd, Water-Reducible and Alkyd Waterborne
	Semi-Gloss – Premium Interior / Exterior Enamel
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd Semi-Gloss  6-1510
	Advance Waterborne Semi-Gloss Alkyd 793

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900 
	Speedhide WB Alkyd Semi-Gloss 6-1510
	Advance Waterborne Semi-Gloss Alkyd 793


	Satin – Premium Interior / Exterior Enamel
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Urethane Alkyd Satin Enamel 7900
	Speedhide WB Alkyd Satin          6-1410
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin Enamel 7900 
	Speedhide WB Alkyd Satin          6-1410
	Aura Grand Entrance Satin 147


			BEHR
	Sherwin-Williams
	Benjamin Moore


16. Steel, Ferrous Metal – High Performance, Industrial Maintenance 
	Semi-Gloss, 100% Acrylic, Direct-To-Metal Enamel
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec  Metal Primer P04

	Intermediate Coat:
	Premium Direct-To-Metal Semi-Gloss 3200
	Pitt-Tech Plus Semi-Gloss DTM 90-1210
	Super Spec HP DTM Semi-Gloss P29

	Topcoat:
	Premium Direct-To-Metal Semi-Gloss 3200
	Pitt-Tech Plus Semi-Gloss DTM 90-1210
	Super Spec HP DTM Semi-Gloss P29



	Gloss, 100% Acrylic, Direct-To-Metal Enamel
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Direct-To-Metal Gloss 8200
	Pitt-Tech Plus Gloss DTM 
90-1310
	Super Spec HP DTM Acrylic Gloss P28

	Topcoat:
	Premium Direct-To-Metal Gloss 8200
	Pitt-Tech Plus Gloss DTM 
90-1310
	Super Spec HP DTM Acrylic Gloss P28



17. Galvanized Metal, Aluminum, and Non-Ferrous Metals
Flat –Premium Interior 100% Acrylic
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat 547

	Topcoat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat 547


	
	Eggshell – Premium Interior 100% Acrylic
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 
9-300Xl
	Regal Select Eggshell 549

	Topcoat:
	Premium Plus Interior Eggshell 2050
	Pure Performance Eggshell 
9-300Xl
	Regal Select Eggshell 549



Satin – Premium Interior 100% Acrylic
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550

	Topcoat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550



	Semi-Gloss – Premium Interior 100% Acrylic
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance  Semi-Gloss 
9-500Xl
	Regal Select Semi-Gloss 551

	Topcoat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance  Semi-Gloss 
9-500Xl
	Regal Select Semi-Gloss 551



	Gloss – Premium Interior 100% Acrylic
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Plus Int/Ext Hi-Gloss 2-8050
	Manor Hall Gloss 52-110
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Int/Ext Hi-Gloss 2-8050
	Manor Hall Gloss 52-110
	Impervex Latex Gloss W309



Flat – Professional, Latex, Interior, Low Odor/VOC
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536

	Topcoat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536



Eggshell – Professional, Latex, Interior, Low Odor/VOC
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell         6-4310XI
	Ultra Spec 500 Eggshell 538

	Topcoat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell         6-4310XI
	Ultra Spec 500 Eggshell 538


			BEHR
	PPG Paints
	         Benjamin Moore


Semi-Gloss – Professional, Latex, Interior, Low Odor/VOC
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Behr Pro Block Filler Primer 50
	Speedhide Block Filler 6-15XI
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss N539

	Topcoat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss N539



18. Galvanized Metal, Aluminum, and Non-Ferrous Metals – Light Industrial Coatings
	Eggshell – Interior Pre-Catalyzed Waterborne Epoxy
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 



	Semi-Gloss – Interior Pre-Catalyzed Waterborne Epoxy
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss



19. Galvanized Metal, Aluminum, and Non-Ferrous Metals – Urethane Alkyd, Water-Reducible and Alkyd Waterborne
	Semi-Gloss – Premium Interior / Exterior Enamel
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd SG 6-1510
	Advance Waterborne Alkyd 793

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900 
	Speedhide WB Alkyd SG 6-1510
	Advance Waterborne Alkyd 793



	Satin – Premium Interior / Exterior Enamel
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Urethane Alkyd Satin 7900
	Speedhide WB Alkyd Satin          6-1410
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin 7900
	Speedhide WB Alkyd Satin          6-1410          
	Aura Grand Entrance Satin 147



20. Galvanized Metal, Aluminum,  Non-Ferrous Metals – High Performance, Industrial Maintenance 
	Semi-Gloss, Premium 100% Acrylic, Direct-To-Metal Enamel
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Direct-To-Metal Semi-Gloss 3200
	Pitt-Tech Plus Semi-Gloss DTM 90-1210
	Super Spec DTM Acrylic Semi-Gloss P29

	Topcoat:
	Premium Direct-To-Metal Semi-Gloss 3200
	Pitt-Tech Plus Semi-Gloss DTM 90-1210
	Super Spec DTM Acrylic Semi-Gloss P29



	
Gloss, Premium 100% Acrylic, Direct-To-Metal Enamel
	Pretreatment:
	Klean Strip Prep & Etch (GKPA30220)
	None recommended.
	Krud Kutter Metal Clean & Etch

	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Premium Direct-To-Metal Gloss 8200
	90-1310 Pitt-Tech Plus Gloss DTM 
	Super Spec DTM Acrylic Gloss P28

	Topcoat:
	Premium Direct-To-Metal Gloss 8200
	90-1310 Pitt-Tech Plus Gloss DTM
	Super Spec DTM Acrylic Gloss P28



			BEHR
	PPG Paints
	Benjamin Moore


21. Galvanized Metal and Non-Ferrous Metals – Dry Fall Coating (Spray applied) 
	Flat, Acrylic / PVA, Dry Fall
	Prime Coat:
	Multi-Surface Primer & Sealer 436
	Pitt-Tech Plus Primer 90-912
	Super Spec Metal Primer P04

	Intermediate Coat:
	Behr Pro Dryfall Flat 890 White, 891 Black 
	Speedhide Dry-Fog Flat 6-275Xl
	Sweep Up Latex Flat 153

	Topcoat:
	Behr Pro Dryfall Flat 890 White, 891 Black
	Speedhide Dry-Fog Flat 6-275Xl
	Sweep Up Latex Flat 153



22. WOOD – Paint Finish
Flat – Premium Interior, Acrylic
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat 547

	Topcoat:
	Premium Plus Interior Flat 1050
	Pure Performance  Flat 9-100
	Regal Select Flat 547



Eggshell – Premium Interior, Acrylic
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Premium Plus Interior Eggshell 2050
	9-300XI Pure Performance  Eggshell
	Regal Select Eggshell 549

	Topcoat:
	Premium Plus Interior Eggshell 2050
	9-300XI Pure Performance  Eggshell
	Regal Select Eggshell 549



Satin – Premium Interior, Acrylic
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550

	Topcoat:
	Premium Plus Interior Satin 7050
	Manor Hall Satin 82-400
	Regal Select Pearl 550



Semi-Gloss – Premium Interior, Acrylic
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance  Semi-Gloss 
9-500Xl
	Regal Select Semi-Gloss 551

	Topcoat:
	Premium Plus Interior Semi-Gloss 3050
	Pure Performance  Semi-Gloss 
9-500Xl
	Regal Select Semi-Gloss 551



Gloss – Premium Interior, Acrylic
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Manor Hall Gloss 52-110
	Impervex Latex Gloss W309

	Topcoat:
	Premium Plus Int/Ext Hi-Gloss2-8050
	Manor Hall Gloss 52-110
	Impervex Latex Gloss W309


(Note: 2-8050 Hi-Gloss Enamel conforms to VOC limits of South Coast AQMD Rule 1113.)

Flat – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536

	Topcoat:
	Behr Pro i300 Interior Flat PR310
	Speedhide Zero Interior Flat 6-4110
	Ultra Spec 500 Int. Flat 536



Eggshell – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell 
6-4310XI
	Ultra Spec 500 Eggshell 538

	Topcoat:
	Behr Pro i300 Interior Eggshell PR330
	Speedhide Zero Interior Eggshell 
6-4310XI
	Ultra Spec 500 Eggshell 538




Semi-Gloss – Professional, Latex, Interior, Low Odor/VOC
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss 539

	Topcoat:
	Behr Pro i300 Interior Semi-Gloss PR370
	Speedhide Zero Interior Semi-Gloss           6-4510XI
	Ultra Spec 500 Semi-Gloss 539


	



			BEHR
	PPG Paints
	Benjamin Moore



23. WOOD – Light Industrial Coating
	Eggshell – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Eggshell HP140 
	Pitt-Glaze 16-310 WB Eggshell Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V342 Pre-Catalyzed Waterborne Epoxy Eggshell 



	Semi-Gloss – Interior Pre-Catalyzed Waterborne Epoxy
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss 

	Topcoat:
	Behr Pro Pre-Catalyzed Waterborne Epoxy Semi-Gloss HP150 
	Pitt-Glaze 16-510 WB Semi-Gloss Pre-Catalyzed Water-Borne Acrylic Epoxy
	Corotech V341 Pre-Catalyzed Waterborne Epoxy Semi-Gloss



24. WOOD – Paint Finish – Urethane Alkyd, Water-Reducible and Alkyd Waterborne
	Semi-Gloss – Premium Interior / Exterior Alkyd (Water-Reducible) Enamel
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Urethane Alkyd Semi-Gloss 3900
	Speedhide WB Alkyd SG 6-1510
	Advance Waterborne Alkyd 793

	Topcoat:
	Urethane Alkyd Semi-Gloss 3900 
	Speedhide WB Alkyd SG 6-1510
	Advance Waterborne Alkyd 793


		
	Satin – Premium Interior / Exterior Alkyd (Water-Reducible) Enamel
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Fresh Start Primer N023

	Intermediate Coat:
	Urethane Alkyd Satin 7900
	Speedhide WB Alkyd Satin 6-1410
	Aura Grand Entrance Satin 147

	Topcoat:
	Urethane Alkyd Satin 7900
	Speedhide WB Alkyd Satin 6-1410
	Aura Grand Entrance Satin 147



	
25. WOOD – Paint Finish – Dry Fall Coating (Spray applied) 
	Flat, Acrylic / PVA, Dry Fall
	Prime Coat:
	Premium All-In-One Primer 75
	Pure Performance Primer 9-900
	Ultra Spec Latex Primer N534

	Intermediate Coat:
	Behr Pro Dryfall Flat 890 White, 891 Black 
	Speedhide Dry-Fog Flat 6-275Xl
	153 Sweep Up Latex Flat

	Topcoat:
	Behr Pro Dryfall Flat 890 White, 891 Black
	Speedhide Dry-Fog Flat 6-275Xl
	153 Sweep Up Latex Flat




END OF SECTION 09 90 00
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